Dedication

I dedicate this dissertation to all my family members, uncle andaunt.

Acknowledgment

Thanks to Allah Almighty for helping me to complete this work. My gratitude is extended to Dr.AdilElhag Ahmed for his wise guidance, which helped me to present this project in this form.

Thanks to my family for their continual support, I am very grateful to the staff of the Department of Chemistry, Sudan University of Science and Technology for all help me.

Abstract

Ferrites of different divalent alkaline earthmetals were synthesized at normal conditions by adopting established co-precipitation method using simple salts of metals. The synthesized ferrite materials includedMagnesium ferrite (Mg-Fer),Calcium ferrite (Ca-Fer),Barium ferrite (Ba-Fer),Strontiumferrite (Sr-Fer)and Iron ferrite (Fe-Fer). These ferrite materials were characterized by various spectroscopic techniques such as Fourier transform infrared spectroscopy(FT-IR), powder X-ray diffraction (XRD)and atomic absorption spectroscopy (AAS). The FT-IR spectroscopic analysis data revealed the presence of Fe-O & M-O bands of respective divalentcationsof cubic spinel structure and absence or low levels of impurities of residual precursors.The XRD analysis results illustrated that the structures of ferrite materials are of cubic single spinel phase. Whereas,the data of AASanalysis indicated the presence of incorporated metallic species, their percentages were found consistent with the empirical formula of normal spinel ferrite MIIFe2O4. This formula is considered the most common form of ferrites of typical spinel structures.

ملخص البحث

تم تحضير مركبات الفيرايتلعدد من فلزات القلويات الأرضية ثنائية الشحنة الموجبةفي الظروف العادية بتبني  طريقه الترسيب المصاحب المعروفه  بإستخدام أملاح بسيطة للفلزات. مركبات الفرايت المحضرة شملت فيرايت المغنزيوم (Mg-Fer)- فيرايت الكالسيوم (Ca-Fer) – فرايتالاسترانشيم (Sr-Fer) و فيرايت الحديد (Fe-Fer). تم تشخيص مواد الفرايت المحضرة عن طريق تقنيات المطيافيه المختلفه مثل مطيافيه الاشعه تحت الحمراء ومطيافيه حيود الاشعه السينيه ومطيافيه الامتصاص الذري.

نتائج تحليل مطيافيه الاشعه تحت الحمراء أظهرت وجود روابط بين الحديد والاكسجين – والمعدن ثنائي الشحنة المقابل والاكسجين لبنية الاسبانيل المكعبة. بينما نتائج تحليل حيود الاشعه السينيه  اوضحت وجود تركيب الاسبانيل المكعب البسيط. بينما دللتالنتائج المتحصل عليها من  مطيافيه الامتصاص الذري وجود المعادن المرتبطة في صيغة الفرايت وقد كانت نسبها متماشيةمع الصيغه الاساسيه لمركبات الفيرايت البسيطة ((MIIFe2O4.وهذه الصيغه تعتبر من اكثر الصيغ المعروفه للفرايت ذات التراكيب الاسباينل .

Contents

| Detection |  |  | I |
| --- | --- | --- | --- |
| Acknowledgment |  |  | II |
| Abstract |  |  | III |
| ملخص البحث |  |  | IV |
| 1 | Classification of ferrites | 2 |  |
| 1.1 | Classification based on magnetic properties | 2 |  |
| 1.1.1 | Soft ferrite | 2 |  |
| 1.1.2 | Hard ferrites of alkaline earth metals | 3 |  |
| 1.2 | Classification according to crystal structure | 3 |  |
| 1.2.1 | Spinel ferrites | 4 |  |
| 1.2.2 | Garnet ferrites | 4 |  |
| 1.2.3 | Ortho ferrites | 4 |  |
| 1.2.4 | Hexagonal ferrites alkaline earth metals | 4 |  |
| 1.3 | Alkali metal ferrites | 6 |  |
| 1.4 | Literature Survey | 7 |  |
|  | Chapter Two (Experimental) |  |  |
| 2.1 | Materials and equipment | 11 |  |
| 2.2 | Synthesis of ferrites | 12 |  |
| 2.2.1 | Synthesis of Iron-ferrite | 12 |  |
| 2.2.2 | Synthesis of Magnesium Ferrite | 12 |  |
| 2.2.3 | Synthesis of calcium Ferrite | 13 |  |
| 2.2.4 | Synthesis of Strontium Ferrite | 13 |  |
| 2.2.5 | Synthesis of Barium Ferrite | 14 |  |
| 2.3 | Characterization Methods | 15 |  |
| 2.3.1 | Fourier Transform Infra-Red spectroscopy | 15 |  |
| 2.3.2 | X-Ray Diffraction (XRD) | 15 |  |
| 2.3.3 | Atomic absorption spectroscopy | 15 |  |
|  | Chapter three (Results and discussion) |  |  |
| 3.1 | Yields of synthesized ferrite | 16 |  |
| 3.2 | Fourier Transform Infra-Red of Ferrites | 17 |  |
| 3.3 | X-ray Diffraction analysis | 22 |  |
| 3.4 | Atomic absorption spectroscopyof samples | 27 |  |
|  | Chapter four ( Conclusions) |  |  |
| 4 | Conclusions | 28 |  |
|  | References | 29 |  |

List of Tables and Figures

| Table 1.1 | Classification of ferrites based on crystal structure | 3 |
| --- | --- | --- |
| Table 1.2 | Subclasses of Hexaferrites | 5 |
| Table 3.1 | The yields of as- the synthesized ferrites | 16 |
| Figure 3.2.1 | IR spectrum of Magnesium Ferrite (Mg-Fer) | 17 |
| Figure 3.2.2 | IR spectrum of calcium Ferrite (Ca-Fer) | 18 |
| Figure 3.2.3 | IR spectrum of Barium Ferrite (Ba-Fer) | 19 |
| Figure 3.2.4 | IR spectrum of Strontium Ferrite (Sr-Fer) | 20 |
| Figure 3.2.5 | IR spectrum of Iron Ferrite (Fe-Fer) | 21 |
| Figure 3.3.1 | X-Ray Diffraction (XRD) pattern of Magnesium Ferrite (Mg-Fer) | 22 |
| Figure 3.3.2 | X-Ray Diffraction (XRD) pattern of Calcium Ferrite(Ca-Fer) | 23 |
| Figure 3.3.3 | X-Ray Diffraction (XRD) pattern of Strontium Ferrite(Sr-Fer) | 24 |
| Figure3.3.4 | X-Ray Diffraction (XRD) pattern of Barium Ferrite (Ba-Fer) | 25 |
| Table 3.4.1 | Atomic absorption analysis | 26 |